#### FM Approvals—Assembly Properties

United Coatings Roof Mate

| Assembly # | Cover Type | Application Type | Securement Type | Deck Type | Wind Uplift | I/Fire | X/Fire | Slope | Hail |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 940-50853-0 | Liquid Applied System | Re-Cover | none | Existing Roof | 90 | 1 | A | 1.5 | SH |
| 213937-50853-0 | Liquid Applied System | Re-Cover | none | Existing Roof | 90 | 1 | A | 1.5 | SH |
| 213939-50853-0 | Liquid Applied System | Re-Cover | none | Existing Roof | 90 | 1 | A | 1.5 | SH |

Hydro-Stop PremiumCoat

| Assembly # | Cover Type | Application Type | Securement Type | Deck Type | Wind Uplift | I/Fire | X/Fire | Slope | Hail |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1076-50822-0 | Liquid Applied System | New Roof | none | Structural Concrete | 105 | NC | A | 1 | SH |
| 1077-50822-0 | Liquid Applied System | New Roof | none | Structural Concrete | 150 | NC | A | 1 | SH |