# ELASTUFF 120

REPAIR PROCEDURE

- Repairs to the coating membrane shall be made either with Elastuff 120 Roller-Grade or Elastuff 120 Mastic, where small spot repairs require a hand-applied material.  Surfaces shall first be roughened using an abrasive brush-blast or by mechanically abrading with a wire wheel, wire brush, coarse sandpaper, or other similar means.  Coating surface must be roughened so as that the repair material is able to achieve a mechanical bond.

- Solvent wipe the surface with M.E.K to remove all dust and other contaminants and to soften the existing coating surface. After thoroughly blending the Part A and B components, apply repair material to the designated area using a brush or mitt, taking care to maintain a flow edge at least 20 mils (508 microns) thick.  Do not feather edges of the repair material.