**Drinking Water System Components**

|  |
| --- |
| [See General Information for Drinking Water System Components](http://database.ul.com/cgi-bin/XYV/template/LISEXT/1FRAME/showpage.html?&name=FDNP.GuideInfo&ccnshorttitle=Drinking+Water+System+Components&objid=1074261552&cfgid=1073741824&version=versionless&parent_id=1073986524&sequence=1) |
|  |  |  |
| **UNITED COATINGS MFR CO** | MH25224 |  |
| 19011 E CATALDO AVE |  |  |
| SPOKANE VALLEY, WA 99016 USA |  |  |

**UL Online Certifications Directory**

**Home Quick Guide Contact Us UL.com**

**FDNP.MH25224**

**Drinking Water System Components**

**ANSI/NSF STANDARD 61**

**Barrier Materials**

|  |  |  |  |
| --- | --- | --- | --- |
| **Trade Dsg** | **Water ContactTemp (°C)** | **Water ContactMtl** | **Surface Area toVolume Ratio** |
|  |  |  |  |
| Elastuff 120 HE (C) | 23 | Polyurethane | 20 sq cm/L |
| Elastuff 120 HE (D) | 82 | Polyurethane | 0.27 sq cm/L |
| Elastuff 120 Mastic (A) | 23 | Polyurethane | 20 sq cm/L |
| Elastuff 120 Mastic (E) | 82 | Polyurethane | 5.0 sq cm/L |
| Elastuff 120 Roller Grade (A) | 23 | Polyurethane | 20 sq cm/L |
| Elastuff 120 Roller Grade (E) | 82 | Polyurethane | 5.0 sq cm/L |
| Elastuff 120 Spray Grade (A) | 23 | Polyurethane | 20 sq cm/L |
| Elastuff 120 Spray Grade (E) | 82 | Polyurethane | 5.0 sq cm/L |
| Uni-Tile Sealer (B) | 82 | Epoxy | 3.40 sq cm/L |

(A) - Tank Size >= 5,000 gal, Maximum Surface Area to Volume Ratio = 20 sq cm/L, Maximum Field Use Dry Film Thickness (mils) = 120, Maximum Thinner = None, Minimum Cure Time = 4 days, Two part coating, mix ratio is 1 Part A to 1 Part B by Volume. See manufacturers instructions for additional product use information. This product was tested without a primer or an additional topcoat. It is recommended that any primer or topcoat used should be certified to ANSI/NSF Standard 61 by an ANSI accredited certifier.

(B) - Tank Size >= 1,000,000 gal, Maximum Surface Area to Volume Ratio = 3.40 sq cm/L, Maximum Field Use Dry Film Thickness (mils) = 7, Maximum Thinner = Up to 2:1 with Technical Grade > 99.5% Pure Acetone, Minimum Cure Time = 7 days, Two part coating, mix ratio is 1 Part A to 1 Part B by Volume.

(C) - Tank Size >= 6000, Maximum Surface Area to Volume Ratio of 20 sq cm/L, only when part A is mixed with Part B in a 1:1 ratio and coated with a maximum thickness of 80 mils

(D) - For use on products where the Surface Area to Volume Ratio does not exceed 0.27 sq cm/L, only when part A is mixed with Part B in a 1:1 ratio and coated with a maximum thickness of 80 mils

(E) - For use on products where the Surface Area to Volume Ratio does not exceed 5.00 sq cm/L, only when part A is mixed with Part B in a 1:1 ratio and coated up to a thickness of 80 mils See manufacturer's instructions for additional product use information.

|  |
| --- |
| Last Updated on 2010-02-18 |

|  |  |  |
| --- | --- | --- |
| [Questions?](http://database.ul.com/cgi-bin/XYV/template/LISEXT/1FRAME/gassist.html) | [Notice of Disclaimer](http://database.ul.com/cgi-bin/XYV/template/LISEXT/1FRAME/gdisclaim.html) | [Page Top](http://database.ul.com/cgi-bin/XYV/template/LISEXT/1FRAME/showpage.html?name=FDNP.MH25224&ccnshorttitle=Drinking+Water+System+Components&objid=1074261815&cfgid=1073741824&version=versionless&parent_id=1073986524&sequence=1" \l "PAGETOP) |

[Copyright © 2010 Underwriters Laboratories Inc.](http://www.ul.com/global/eng/pages/corporate/onlinepolicies/copyrightnotice/)®

The appearance of a company's name or product in this database does not in itself assure that products so identified have been manufactured under UL's Follow-Up Service. Only those products bearing the UL Mark should be considered to be Listed and covered under UL's Follow-Up Service. Always look for the Mark on the product.

UL permits the reproduction of the material contained in the Online Certification Directory subject to the following conditions: 1. The Guide Information, Designs and/or Listings (files) must be presented in their entirety and in a non-misleading manner, without any manipulation of the data (or drawings). 2. The statement "Reprinted from the Online Certifications Directory with permission from Underwriters Laboratories Inc." must appear adjacent to the extracted material. In addition, the reprinted material must include a copyright notice in the following format: "Copyright © 2010 Underwriters Laboratories Inc.®"