Date:	7/31/26

Elastuff 101/102 Permeance Testing

Permeance Testing was done in accordance with ASTM D-1653 Test Method B (Wet Cup), condition A  (50% RH, 23° C).

Sample specimens were prepared as multiple drawdown passes on Lenetta Release Paper to give a final film thickness of 10-12 dry mils.

Testing was done on the following systems:

Elastuff 101 only, Batch number 92061

Elastuff 102 only, Batch number 91207

Elastuff 101/ Elastuff 102 System

Permeance Results:

| Sample | Thickness (mils) | Permeance (grams/meter2 24 Hours mm Hg) |
| --- | --- | --- |
| Elastuff 101 Only | 12 | 2.15 |
| Elastuff 101/102 System | 24 | 1.68 |
| Elastuff 102 Only | 10.5 | 1.74 |