Date: 6/28/02

File #: NA

Customer: Bill Mann

Application: China

Subject: Elastuff 160 resistance to Sea Water

Objective: Same as above

Procedure: A 3 day and 30 day immersion (using free film) was performed at 25 degrees C.

Results:

Elastuff 160 has less than a 1% swell at 30 days immersion.

30 Day					3 Day

| 1.3796 | 1.3865 | 0.50% |  | 1.3796 | 1.3845 | 0.36% |
| --- | --- | --- | --- | --- | --- | --- |
| 1.2753 | 1.2818 | 0.51% |  | 1.2753 | 1.2803 | 0.39% |
| 1.3530 | 1.3605 | 0.55% |  | 1.3530 | 1.3591 | 0.45% |

Discussion: This data comes from the testing completed on 6/27/02.  Mr. Heinje and I are in consensus that this exceeds the needs for continuous immersion service at this temperature.  This data also indicates immersion service up to 50 degrees C. is expected.  Any questions or comments are appreciated.

Prepared By:

Tony Drager

Research

tony@unitedcoatings.com

(509) 926-7143 ext. 156

Steve Heinje

Technical Director

heinje@unitedcoatings.com

(509) 926-7143 ext. 113