05/27/04

Project:

Elastuff 160 CR Version Tear Strength

Purpose:

Determine Tear Strength properties of Elastuff 160 Corrosion Resistant

Products:

Elastuff 160 CR

Procedures:

Samples were tested in accordance with ASTM D-624 Die “C”. Testing instrument: Shimadzu AG-I.  Temperature 77°F (25°C)

Key Results:

— Tear Strength Values —

|  | #### Tear Strength pounds/inch |
| --- | --- |
| Sample 1 | 403 |
| Sample 2 | 443 |
| Sample 3 | 384 |
| Sample 4 | 450 |
| Sample 5 | 430 |
| Average | 422 (+/-25) |

Conclusion:

Average Tear Strength value for the five samples of Elastuff 160 CR was found to be 422 pounds/inch (+/- 25)  (74(+/-4) kN/m)

Prepared by:

Mike Sand

Lead Chemist

mike@unitedcoatings.com

(509) 926-7143 ext. 135