09-07-04

### File #: SF 0542

Project:

Evaluation of impact properties of Elastuff 160 CR.

| Gardner Impact |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Product Name | Elastuff 160 CR |  |  |  |  |  |  |  |
| Batch Number | Part A: 98483, Part B: 98330 |  |  |  |  |  |  |  |
| Manufacture Date | Part A: 8-19-2004, Part B: 7-27-2004 |  |  |  |  |  |  |  |
| Test Date | 7 Sept 04 |  |  |  |  |  |  |  |
| Application/Date | 26 August 04 / 160o F. material temperature at 2500 psi pump pressure |  |  |  |  |  |  |  |
| Test Method | ASTM D-2794 Standard Test Method for Resistance of Organic Coatings to the effects of Rapid Deformation |  |  |  |  |  |  |  |
| Test temperature | 23°C |  |  |  |  |  |  |  |
| This certificate confirms that the above product was tested as per stated standard |  |  |  |  |  |  |  |  |
| Specification using calibrated equipment and qualified staff. The following test results |  |  |  |  |  |  |  |  |
| were obtained. |  |  |  |  |  |  |  |  |
| Test Results |  |  |  |  |  |  |  |  |
| Impact Resistance |  |  |  |  | Inch-Pounds |  | Pass/Fail |  |
| Intrusion |  |  |  |  | 160 (1.8 kg-m) |  | Pass |  |
| Extrusion |  |  |  |  | 57 (0.63 kg-m) |  | Pass |  |
| Test conditions (if different from standard test conditions) and/or notes. |  |  |  |  |  |  |  |  |
| Indenter: 4 pound steel punch with .625" hemispherical head. |  |  |  |  |  |  |  |  |
| Average coating thickness: .048" (12mm) |  |  |  |  |  |  |  |  |
| Substrate: Steel Thickness: .12" (30mm) |  |  |  |  |  |  |  |  |
| Coatings applied to steel panels using Graco plural component proportioning system. |  |  |  |  |  |  |  |  |