11-19-2003

### File #: SF0540

##### Research Test Report

Project:

Elastuff 160 properties testing, Adhesion

Procedures:

Elastuff 160 was spray applied to “white” blasted steel panels.

Cure period consisted of 2 weeks at ambient (18-23°C) temperatures.

Samples were tested in accordance with ASTM D-4541.

Testing instrument: Deflesco Positest Adhesion Tester..

Key Results:

— Adhesion Values —

| Sample ID | #### Pull Strength pounds/inch | #### Adhesion Failure Type |
| --- | --- | --- |
| Sample 1 | 2550 | Coating cohesive |
| Sample 2 | 2800 | Coating cohesive |
| Sample 3 | 1800 | Dolly Adhesive |
| Sample 4 | 2400 | Coating cohesive |
| Average | 2387 |  |

Conclusion:

Average Adhesion of Elastuff 160 to steel panel exceeded a minimum of 2300 psi as failure occurred as coating cohesive failure before any coating-steel bond breakage was achieved.