07-07-2004

### File #: SF0540

##### Research Test Report

Project:

Elastuff 160 Properties Testing, Tensile/Elongation

Procedure:

Samples from sprayed free films of Elastuff 160 were tested in accordance with ASTM D412, DIE C with a crosshead speed 20 inches/minute.

Part A:  Elastuff 160 Part A Clear Batch # 97473

Part B:  Elastuff 160 Part B Light Gray Batch #97475

Results:

| Sample ID | Film thickness Inches | Film Width Inches | Maximum Force # |  | Tensile #’s/sq in | Elongation % |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.0340 | 0.25 | 36.0 |  | 4,235 | 20% |
| 2 | 0.0355 | 0.25 | 36.0 |  | 4,056 | 15% |
| 3 | 0.0320 | 0.25 | 32.0 |  | 4,000 | 25% |
| 4 | 0.0405 | 0.25 | 38.0 |  | 3,753 | 15% |
| AVERAGE |  |  |  |  | 4,011 | 19% |